## PROWEST   CO., LTD.

Corporate  Overview

The company produces a comprehensive range of heat shrinkable tubing in various kinds of colours and shrink ratio. They are to UL224/CSA approvals and all products are backed by our ISO 9001 Quality Systems. As Sony’s Green Partner, our products not only can meet Sony environment substance requirements, but also ROHS compliance.

Our market share has dramatically increased both at home and abroad since the Year 2000, which has been contributed mainly by its product quality and reputation. Today, PROWEST enjoys a good reputation for exporting best quality heat shrinkable tubing to Europe, North America, Australia, and South East Asia.

“Sincerity, Practically, Innovation, Challenge and Perfection” are our corporate culture; providing better co-operation with mutual benefits and excellent customer services are our company goal; manufacturing safe, reliable and innovative new products are our management pursuits.

### Changyuan products

Tubing

| Product Name | General Description | Max. Operating Temperature | Potential Rating | Shrink ratio | Available Colors | Page |
| --- | --- | --- | --- | --- | --- | --- |
| CB-HFT | Flexible, Flam-retardant, UL(125℃),VW-1 No.198.1 Fmark | 125℃ | 600V | 2:1 | All colors except clear | 3-4 |
| CB-TW | Thin wall, flexible, flame-retardant, Fmark | 125℃ | 300v | 2:1 | All colors except clear | 5 |
| CB-DWT | Flexible, Flam-retardant, Adhesive coated UL224, CSA No.198.1,Fmark | 125℃ | 600V | 2:1 3:1 4:1 | All colors | 6-8 |
| CB-YGT | Flexible, Flam-retardant, UL(125℃),VW-1 No.198.1 Fmark | 125℃ | 300V/600V | 2:1 | Yellow/green | 9-10 |
| CB-GSRT(3X) | Great shrink ratio UL224, CSA No.198.1 | 125℃ | 300V/600V | 3:1 | All colors | 11 |
| CB-HRT | Corrosion resistant, heat-resistant No.198.1 Fmark | 150℃ | 300V/600V | 2:1 | All colors | 12-13 |
| CB-TT | PTFE UL Fmark | 200℃ | 300V/600V | 1:1 | All colors | 14-15 |
| CB-300/ CB-600 | PVC non-shrinkable | 105℃ | 300V/600V | 1:1 | All colors | 16-17 |
| CB-PET | UL 224 | 130℃ | 600V | 2:1 | All colors | 18 |
| CB-101 | General prupose Non-flame retardant | 105℃ | 600V/300V | 2:1 | Clear | 19-20 |
| CB-301 | Non-flame retardant | 105℃ | 600V | 2:1 | All colors | 21-22 |
| CB-150 | Flam-retardant | 150℃ | 600V | 2:1 | Clear | 23-24 |
| CB-175 | Flam-retardant | 175℃ | 600V | 2:1 | Clear | 25-26 |
| CB-2000 | Semi-rigid SAE-AMS-DTL-23053 | 125℃ | 600V | 1.5:1 | Black | 27 |
| CB-ULTHST | Ultea low temp heat-shrinkable | 42℃ | 600V | 1.5:1 | All colors except Clear | 28 |

###### CB-HFT

###### HALOGEN FREE HEAT－SHRINKABLE TUBING

CB-HFT is a halogen-free low smok, flexible, flame retardant heat-shrinkable tubing. This tubing is free of Pb,Cd, Hg,Cr+6, PBB and PBDE.CB-HFT can be used in any enclosed area where a flame-retardant, halogen-free enviroment is requiedThe product is UL recognized and the file No is E180908, All are F mark.

Specifications

| Item |  | Specifications |
| --- | --- | --- |
| Shrink Temperature (℃) |  | 90 |
| Temperature Range (℃) |  | 125 |
| Radial Shrinking Ratio (%) |  | ≥50 |
| Longitudinal Change (%) |  | ≤5 |
| Tensile Strength (Mpa) |  | ≥10.4 |
| Ultimate Elongation (%) |  | ≥200 |
| Aging in Circulating-air Oven |  | 158.0±1.0℃, 168hrs |
| After aging | Tensile Strength (Mpa) | ≥7.3 |
|  | Ultimate Elongation (%) | ≥100 |
| Volume Resistivity (Ω cm) |  | ≥1014 |
| Dielectric Strength (KV/mm) |  | ≥15 |
| Flammability |  | VW-1 |
| Concentricity (%) |  | ≥65 |

Size

| Size | As Supplied (mm) |  | After Recovery (mm) |  |
| --- | --- | --- | --- | --- |
|  | Inside Diameter | Wall-thickness | Inside Diameter | Wall-thickness |
| φ0.8 | 1.3±0.2 | 0.15±0.05 | ≤0.45 | 0.28±0.05 |
| φ1.0 | 1.5±0.2 | 0.18±0.05 | ≤0.6 | 0.30±0.05 |
| φ1.5 | 2.0±0.2 | 0.18±0.05 | ≤0.8 | 0.32±0.05 |
| φ2.0 | 2.5±0.2 | 0.18±0.05 | ≤1.00 | 0.35±0.05 |
| φ2.5 | 3.0±0.2 | 0.20±0.05 | ≤1.25 | 0.38±0.05 |
| φ3.0 | 3.5±0.3 | 0.20±0.05 | ≤1.5 | 0.38±0.05 |
| φ3.5 | 4.0±0.3 | 0.20±0.05 | ≤1.75 | 0.38±0.05 |
| φ4.0 | 4.5±0.3 | 0.23±0.05 | ≤2.0 | 0.45±0.05 |
| φ4.5 | 4.8±0.3 | 0.23±0.05 | ≤2.25 | 0.45±0.05 |
| φ5.0 | 5.5±0.3 | 0.23±0.05 | ≤2.5 | 0.45±0.05 |
| φ6.0 | 6.5±0.4 | 0.25±0.05 | ≤3.0 | 0.50±0.05 |
| φ6.5 | 7.0±0.4 | 0.25±0.05 | ≤3.0 | 0.52±0.05 |
| φ7.0 | 7.5±0.4 | 0.30±0.08 | ≤3.5 | 0.60±0.05 |
| φ8.0 | 8.5±0.3 | 0.30±0.08 | ≤4.0 | 0.60±0.08 |
| φ9.0 | 9.5±0.4 | 0.30±0.08 | ≤4.5 | 0.60±0.08 |
| φ10 | 10.5±0.5 | 0.30±0.08 | ≤5.0 | 0.60±0.08 |
| φ11 | 11.5±0.5 | 0.30±0.08 | ≤5.5 | 0.60±0.08 |
| φ12 | 12.5±0.5 | 0.30±0.08 | ≤6.0 | 0.60±0.08 |
| φ13 | 13.5±0.5 | 0.36±0.12 | ≤6.5 | 0.65±0.12 |
| φ14 | 14.5±0.5 | 0.36±0.12 | ≤7.0 | 0.65±0.12 |
| φ15 | 15.5±0.5 | 0.36±0.12 | ≤7.5 | 0.65±0.12 |
| φ16 | 16.5±0.5 | 0.36±0.12 | ≤8.0 | 0.70±0.12 |
| φ17 | 17.5±0.5 | 0.36±0.12 | ≤8.5 | 0.70±0.12 |
| φ18 | 18.7±0.5 | 0.40±0.15 | ≤9.0 | 0.75±0.12 |
| φ20 | 20.6±0.6 | 0.40±0.15 | ≤10.0 | 0.80±0.12 |
| φ22 | 22.7±0.6 | 0.40±0.15 | ≤11.0 | 0.80±0.12 |
| φ25 | 25.5±0.7 | 0.45±0.15 | ≤12.5 | 0.90±0.12 |
| φ28 | 29.2±0.7 | 045±0.15 | ≤14.0 | 0.90±0.12 |
| φ30 | 31.0±0.7 | 0.45±0.15 | ≤15.0 | 0.90±0.12 |
| φ35 | ≥35 | 0.50±0.15 | ≤19 | 1.00±0.30 |
| φ40 | ≥40 | 0.50±0.15 | ≤21 | 1.00±0.30 |
| φ50 | ≥50 | 0.50±0.15 | ≤27 | 1.00±0.30 |
| φ55 | ≥55 | 0.50±0.15 | ≤28 | 1.00±0.30 |
| φ60 | ≥60 | 0.50±0.15 | ≤31 | 1.00±0.30 |

Size in Inch

| SIZE (in inch) | As supplied in mm |  | After Recovery (mm) |  |
| --- | --- | --- | --- | --- |
|  | MIN ID (in mm) | WALL (in mm) | MIN ID (in mm) | WALL (in mm) |
| 3/64 | 1.2 | 0.18±0.05 | ≤0.6 | 0.30±0.05 |
| 1/16 | 1.6 | 0.18±0.05 | ≤0.8 | 0.32±0.05 |
| 3/32 | 2.4 | 0.18±0.05 | ≤1.00 | 0.35±0.05 |
| 1/8 | 3.2 | 0.20±0.05 | ≤1.5 | 0.38±0.05 |
| 3/16 | 4.8 | 0.23±0.05 | ≤2.0 | 0.45±0.05 |
| 1/4 | 6.4 | 0.25±0.05 | ≤3.0 | 0.50±0.05 |
| 3/8 | 9.5 | 0.30±0.08 | ≤4.5 | 0.60±0.08 |
| 1/2 | 12.7 | 0.30±0.08 | ≤6.0 | 0.60±0.08 |
| 3/4 | 19.1 | 0.40±0.12 | ≤10.0 | 0.75±0.12 |
| 1 | 25.4 | 0.45±0.12 | ≤12.5 | 0.90±0.12 |
| 1–1/4 | 31.8 | 0.45±0.12 | ≤15.0 | 0.90±0.12 |
| 1–1/2 | 38.1 | 0.50±0.15 | ≤21 | 1.00±0.30 |
| 2 | 50.8 | 0.50±0.15 | ≤27 | 1.00±0.30 |

Other sizes are available upon special order.

CB- TW

CB- TW HEAT－SHRINKABLE TUBING

CB-TW tubing is a kind of thin-wall, flame-retardant polyolefin heat-shrinkable tubing and free of Pb,Cd, Hg,Cr+6, PBB and PBDE .The tubing are designed for the applications that require an ultra thin wall for rapid shrinking. The products are UL recognized at 125℃, 300V. All are F mark.

Size

| Size | As Supplied（mm） |  | After Recovery（mm） |  |
| --- | --- | --- | --- | --- |
|  | Inside Diameter | Wall-thickness | Inside Diameter | Wall-thickness |
| φ0.8 | 1.1±0.2 | 0.10±0.05 | ≤0.45 | 0.22±0.02 |
| φ1.0 | 1.5±0.3 | 0.10±0.05 | ≤0.6 | 0.22±0.05 |
| φ1.5 | 2.0±0.3 | 0.10±0.03 | ≤0.8 | 0.22±0.05 |
| φ2.0 | 2.5±0.3 | 0.10±0.05 | ≤1.0 | 0.22±0.05 |
| φ2.5 | 3.0±0.3 | 0.13±0.05 | ≤1.25 | 0.25±0.05 |
| φ3.0 | 3.5±0.4 | 0.13±0.05 | ≤1.5 | 0.28±0.05 |
| φ3.5 | 4.0±0.4 | 0.13±0.05 | ≤1.75 | 0.30±0.05 |
| φ4.0 | 4.5±0.4 | 0.15±0.05 | ≤2.0 | 0.32±0.05 |
| φ5.0 | 5.5±0.4 | 0.15±0.05 | ≤2.5 | 0.32±0.05 |
| φ6.0 | 6.5±0.4 | 0.15±0.05 | ≤3.0 | 0.32±0.05 |
| φ7.0 | 7.5±0.4 | 0.15±0.05 | ≤3.5 | 0.32±0.05 |
| φ8.0 | 8.5±0.5 | 0.15±0.05 | ≤4.0 | 0.32±0.05 |
| φ9.0 | 9.5±0.5 | 0.16±0.05 | ≤4.5 | 0.36±0.05 |
| φ10 | 10.5±0.5 | 0.16±0.05 | ≤5.0 | 0.36±0.05 |
| φ11 | 11.5±0.5 | 0.18±0.05 | ≤5.5 | 0.36±0.05 |
| φ12 | 12.5±0.5 | 0.18±0.05 | ≤6.0 | 0.36±0.05 |
| φ13 | 13.5±0.5 | 0.18±0.05 | ≤6.5 | 0.36±0.05 |
| φ14 | 14.5±0.5 | 0.18±0.05 | ≤7.0 | 0.36±0.05 |
| φ15 | 15.5±0.5 | 0.18±0.05 | ≤7.5 | 0.36±0.05 |

Size in Inch

| SIZE (in inch) | As supplied in mm |  | After Recovery (mm) |  |
| --- | --- | --- | --- | --- |
|  | MIN ID (in mm) | WALL (in mm) | MIN ID (in mm) | WALL (in mm) |
| 3/64 | 1.2 | 0.10±0.05 | ≤0.6 | 0.22±0.03 |
| 1/16 | 1.6 | 0.10±0.05 | ≤0.75 | 0.22±0.03 |
| 3/32 | 2.4 | 0.10±0.05 | ≤1.0 | 0.22±0.05 |
| 1/8 | 3.2 | 0.13±0.05 | ≤1.5 | 0.25±0.05 |
| 3/16 | 4.8 | 0.15±0.05 | ≤2.5 | 0.32±0.05 |
| 1/4 | 6.4 | 0.15±0.05 | ≤3.0 | 0.32±0.05 |
| 3/8 | 9.5 | 0.16±0.05 | ≤4.5 | 0.36±0.05 |
| 1/2 | 12.7 | 0.18±0.05 | ≤6.0 | 0.36±0.05 |

###### CB-DWT

###### DUAL-WALL HEAT－SHRINKABLE TUBING

CB-DWT is coated with adhesive and  free of Pb,Cd, Hg,Cr+6, PBB and PBDE.CB-DWT are widely used in  electrical applications, including water-proff and sealing.High expansion ratio makes it possible to repair most damaged cable jackets without removing connectors. The product is UL recognized and the file No is E180908.

All are F mark.

Specifications

| Items |  | ###### Specifications |
| --- | --- | --- |
| Shrink Temperature(℃) |  | 110 |
| Operating Temperature Range(℃) |  | -55—125 |
| Tensile Strength (Mpa) |  | ≥10.4 |
| Ultimate Elongation (%) |  | ≥200 |
| Radial shrinking ratio (%) |  | ≥50 |
| Longitudinal Change (%) |  | ≤10 |
| Aging in Circulating-air Oven |  | 158.0±1.0℃, 168hrs |
| After Aging | Tensile Strength (Mpa) | ≥7.3 |
|  | Ultimate Elongation (%) | ≥100 |
| Dielectric Strength (kV/mm) |  | ≥15.0 |
| Volume Resistivity (Ω cm) |  | ≥1013 |
| Flammability |  | VW-1 |
| Water Absorption (%) |  | Less than 0.4% |
| Fluid Resistance |  | Excellent |
| (Copper Corrosion) |  | (No Corrosion) |
| Softening Point (℃) |  | 120±5 |
| Tissue Strength (N/25mm) |  | >80 |

Specifications of Heat-shrinkable Dual-wall Tubing

a．CB_DWT (2X)

| Size (IN) | As Supplied |  |  |  | After Recovery |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Min ID |  | Nominal Wall Thickness |  | Max ID |  | Total Wall Thickness |  | Nominal Adhesive Wall |  |
|  | mm | IN | mm | IN | mm | IN | mm | IN | mm | IN |
| 3/64 | 1.2 | 0.047 | 0.30 | 0.012 | 0.6 | 0.024 | 0.45±0.12 | 0.018±.005 | 0.20 | 0.008 |
| 1/16 | 1.6 | 0.062 | 0.30 | 0.012 | 0.8 | 0.031 | 0.45±0.12 | 0.018±.005 | 0.20 | 0.008 |
| 3/32 | 2.4 | 0.093 | 0.35 | 0.014 | 1.2 | 0.046 | 0.55±0.12 | 0.022±.005 | 0.30 | 0.012 |
| 1/8 | 3.2 | 0.125 | 0.4 | 0.016 | 1.60 | 0.062 | 0.60±0.15 | 0.027±.006 | 0.30 | 0.012 |
| 3/16 | 4.8 | 0.187 | 0.4 | 0.016 | 2.4 | 0.093 | 0.75±0.15 | 0.029±.006 | 0.35 | 0.014 |
| 1/4 | 6.4 | 0.250 | 0.4 | 0.016 | 3.20 | 0.125 | 0.75±0.15 | 0.029±.006 | 0.35 | 0.014 |
| 3/8 | 9.5 | 0.375 | 0.4 | 0.016 | 4.80 | 0.187 | 0.80±0.20 | 0.032±.008 | 0.35 | 0.014 |
| 1/2 | 12.7 | 0.500 | 0.4 | 0.016 | 6.40 | 0.250 | 0.80±0.20 | 0.032±.008 | 0.35 | 0.014 |
| 3/4 | 19.1 | 0.750 | 0.5 | 0.020 | 9.50 | 0.375 | 0.95±0.28 | 0.037±.011 | 0.40 | 0.017 |
| 1 | 25.4 | 1.000 | 0.5 | 0.020 | 12.7 | 0.500 | 1.15±0.28 | 0.045±.011 | 0.45 | 0.017 |
| 1 -1/2 | 38.1 | 1.500 | 0.65 | 0.025 | 19.00 | 0.750 | 1.25±0.41 | 0.049±.016 | 0.45 | 0.017 |
| 2 | 50.8 | 2.000 | 0.73 | 0.029 | 25.4 | 1.000 | 1.40±0.41 | 0.055±.016 | 0.50 | 0.019 |

b．CB-DWT (3X)

| Size (IN) | As Supplied |  |  |  | After Recovery |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Min ID |  | Nominal Wall Thickness |  | Max ID |  | Total Wall Thickness |  | Nominal Adhesive Wall |  |
|  | mm | IN | mm | IN | mm | IN | mm | IN | mm | IN |
| 1/8 | 3 | 0.118 | 0.57 | 0.022 | 1 | 0.039 | 1.00±.28 | 0.039±.010 | 0.50 | 0.020 |
| 3/16 | 4.8 | 0.187 | 0.57 | 0.022 | 1.5 | 0.06 | 1.0±.28 | 0.039±.010 | 0.60 | 0.025 |
| 1/4 | 6 | 0.236 | 0.57 | 0.022 | 2 | 0.079 | 1.00±.28 | 0.039±.010 | 0.50 | 0.020 |
| 3/8 | 9 | 0.354 | 0.64 | 0.025 | 3 | 0.118 | 1.40±.28 | 0.055±.010 | 0.61 | 0.024 |
| 1/2 | 12 | 0.472 | 0.80 | 0.031 | 4 | 0.157 | 1.78±.38 | 0.070±.010 | 0.76 | 0.030 |
| 3/4 | 19 | 0.748 | 0.93 | 0.036 | 6 | 0.236 | 2.25±.55 | 0.088±.020 | 0.76 | 0.030 |
| 1 | 24 | 0.940 | 1.00 | 0.040 | 8 | 0.315 | 2.54±.55 | 0.100±.020 | 1.02 | 0.040 |
| 1 1/4 | 31.8 | 1.252 | 1.00 | 0.040 | 11 | 0.433 | 2.54±.55 | 0.100±.020 | 1.02 | 0.040 |
| 1 -1/2 | 38.1 | 1.570 | 1.00 | 0.040 | 13 | 0.512 | 2.54±.55 | 0.100±.020 | 1.02 | 0.040 |
| 2 | 50 | 1.890 | 1.00 | 0.040 | 17 | 0.669 | 2.54±.55 | 0.100±.020 | 1.02 | 0.040 |

c. CB-DWT (4X)

| Size (IN) | As Supplied（Expanded） |  |  |  | After Recovery（Recovered） |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Min ID |  | Nominal Wall Thickness |  | Max ID |  | Total Wall Thickness |  | Nominal Adhesive Wall |  |
|  | mm | IN | mm | IN | mm | IN | mm | IN | mm | IN |
| 1/4 | 4 | 0.157 | 0.40 | 0.016 | 1 | 0.039 | 1.00±0.28 | 0.039±0.010 | 0.50 | 0.020 |
| 8/2 | 8 | 0.315 | 0.40 | 0.016 | 2 | 0.079 | 1.10±0.28 | 0.039±0.010 | 0.50 | 0.020 |
| 12/3 | 12 | 0.472 | 0.50 | 0.020 | 3 | 0.118 | 1.40±0.28 | 0.055±0.010 | 0.61 | 0.024 |
| 16/4 | 16 | 0.630 | 0.60 | 0.024 | 4 | 0.157 | 1.78±0.38 | 0.070±0.010 | 0.76 | 0.030 |
| 24/6 | 24 | 0.945 | 0.75 | 0.030 | 6 | 0.236 | 2.25±0.55 | 0.088±0.020 | 0.76 | 0.030 |
| 32/8 | 32 | 1.260 | 0.80 | 0.031 | 8 | 0.315 | 2.54±0.55 | 0.100±0.020 | 1.02 | 0.040 |
| 52/13 | 52 | 2.050 | 0.80 | 0.031 | 13 | 0.512 | 2.60±0.55 | 0.100±0.020 | 1.02 | 0.040 |

Specifications of Heat-shrinkable Dual-wall Tubing (Thin Wall)

CB-DWT-T (2X)

| Size (IN) | As Supplied |  |  |  | After Recovery |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Min ID |  | Nominal Wall Thickness |  | Max ID |  | Total Wall Thickness |  | Nominal Adhesive Wall |  |
|  | mm | IN | mm | IN | Mm | IN | mm | IN | mm | IN |
| 3/64 | 1.2 | 0.047 | 0.22 | 0.008 | 0.6 | 0.024 | 0.35±.12 | 0.014±.005 | 0.15 | 0.006 |
| 1/16 | 1.6 | 0.062 | 0.22 | 0.008 | 0.8 | 0.031 | 0.35±.12 | 0.014±.005 | 0.15 | 0.006 |
| 3/32 | 2.4 | 0.093 | 0.28 | 0.011 | 1.2 | 0.046 | 0.45±.12 | 0.017±.005 | 0.20 | 0.008 |
| 1/8 | 3.2 | 0.125 | 0.30 | 0.012 | 1.60 | 0.062 | 0.50±.15 | 0.019±.006 | 0.20 | 0.008 |
| 3/16 | 4.8 | 0.187 | 0.30 | 0.012 | 2.4 | 0.093 | 0.50±.15 | 0.019±.006 | 0.20 | 0.008 |
| 1/4 | 6.4 | 0.250 | 0.35 | 0.014 | 3.20 | 0.125 | 0.65±.15 | 0.026±.006 | 0.20 | 0.008 |
| 3/8 | 9.5 | 0.375 | 0.35 | 0.014 | 4.80 | 0.187 | 0.65±.28 | 0.026±.011 | 0.25 | 0.010 |
| 1/2 | 12.7 | 0.500 | 0.35 | 0.014 | 6.40 | 0.250 | 0.65±.28 | 0.026±.011 | 0.25 | 0.010 |
| 3/4 | 19.1 | 0.750 | 0.40 | 0.016 | 9.50 | 0.375 | 0.75±.28 | 0.030±.011 | 0.25 | 0.010 |
| 1 | 25.4 | 1.000 | 0.40 | 0.016 | 12.7 | 0.500 | 0.77±.28 | 0.030±.011 | 0.30 | 0.012 |
| 1 -1/2 | 38.1 | 1.500 | 0.52 | 0.020 | 19.00 | 0.750 | 1.00±.41 | 0.040±.016 | 0.30 | 0.012 |
| 2 | 50.8 | 2.000 | 0.52 | 0.020 | 25.4 | 1.000 | 1.00±.41 | 0.040±.016 | 0.30 | 0.012 |

Other sizes are available upon special order.

###### CB-YGT

###### YELLOW/GREEN STRIPED HEAT-SHRINKABLE TUBING

CB-YGT is a yellow and green striped heat-shrinkable tubing which is flexible, flame-retardant and resistant to common fluids and solvents.  This tubing may be used in yellow and green wiring linkage and ground marking. This tubing is free of Pb,Cd, Hg,Cr+6, PBB and PBDE nd Ul approved. All are F mark.

Size

| Size | As Supplied (mm) |  | After Recovery (mm) |  |
| --- | --- | --- | --- | --- |
|  | Inside Diameter | Wall-thickness | Inside Diameter | Wall-thickness |
| φ2.0 | 2.5±0.2 | 0.18±0.05 | ≤1.00 | 0.35±0.05 |
| φ2.5 | 3.0±0.2 | 0.20±0.05 | ≤1.25 | 0.38±0.05 |
| φ3.0 | 3.5±0.3 | 0.20±0.05 | ≤1.5 | 0.38±0.05 |
| φ3.5 | 4.0±0.3 | 0.20±0.05 | ≤1.75 | 0.38±0.05 |
| φ4.0 | 4.5±0.3 | 0.23±0.05 | ≤2.0 | 0.45±0.05 |
| φ4.5 | 4.8±0.3 | 0.23±0.05 | ≤2.25 | 0.45±0.05 |
| φ5.0 | 5.5±0.3 | 0.23±0.05 | ≤2.5 | 0.45±0.05 |
| φ6.0 | 6.5±0.4 | 0.25±0.05 | ≤3.0 | 0.50±0.05 |
| φ6.5 | 7.0±0.4 | 0.25±0.05 | ≤3.0 | 0.52±0.05 |
| φ7.0 | 7.5±0.4 | 0.30±0.08 | ≤3.5 | 0.60±0.05 |
| φ8.0 | 8.5±0.3 | 0.30±0.08 | ≤4.0 | 0.60±0.08 |
| φ9.0 | 9.5±0.4 | 0.30±0.08 | ≤4.5 | 0.60±0.08 |
| φ10 | 10.5±0.5 | 0.30±0.08 | ≤5.0 | 0.60±0.08 |
| φ11 | 11.5±0.5 | 0.30±0.08 | ≤5.5 | 0.60±0.08 |
| φ12 | 12.5±0.5 | 0.30±0.08 | ≤6.0 | 0.60±0.08 |
| φ13 | 13.5±0.5 | 0.36±0.12 | ≤6.5 | 0.65±0.12 |
| φ14 | 14.5±0.5 | 0.36±0.12 | ≤7.0 | 0.65±0.12 |
| φ15 | 15.5±0.5 | 0.36±0.12 | ≤7.5 | 0.65±0.12 |
| φ16 | 16.5±0.5 | 0.36±0.12 | ≤8.0 | 0.70±0.12 |
| φ17 | 17.5±0.5 | 0.36±0.12 | ≤8.5 | 0.70±0.12 |
| φ18 | 18.7±0.5 | 0.40±0.15 | ≤9.0 | 0.75±0.12 |
| φ20 | 20.6±0.6 | 0.40±0.15 | ≤10.0 | 0.80±0.12 |
| φ22 | 22.7±0.6 | 0.40±0.15 | ≤11.0 | 0.80±0.12 |
| φ25 | 25.5±0.7 | 0.45±0.15 | ≤12.5 | 0.90±0.12 |
| φ28 | 29.2±0.7 | 045±0.15 | ≤14.0 | 0.90±0.12 |
| φ30 | 31.0±0.7 | 0.45±0.15 | ≤15.0 | 0.90±0.12 |

Size in Inch

| SIZE (in inch) | As supplied in mm |  | After Recovery (mm) |  |
| --- | --- | --- | --- | --- |
|  | MIN ID (in mm) | WALL (in mm) | MIN ID (in mm) | WALL (in mm) |
| 3/32 | 2.4 | 0.18±0.05 | ≤1.00 | 0.35±0.05 |
| 1/8 | 3.2 | 0.20±0.05 | ≤1.5 | 0.38±0.05 |
| 3/16 | 4.8 | 0.23±0.05 | ≤2.0 | 0.45±0.05 |
| 1/4 | 6.4 | 0.25±0.05 | ≤3.0 | 0.50±0.05 |
| 3/8 | 9.5 | 0.30±0.08 | ≤4.5 | 0.60±0.08 |
| 1/2 | 12.7 | 0.30±0.08 | ≤6.0 | 0.60±0.08 |
| 3/4 | 19.1 | 0.40±0.12 | ≤10.0 | 0.75±0.12 |
| 1 | 25.4 | 0.45±0.12 | ≤12.5 | 0.90±0.12 |
| 1 1/4 | 31.8 | 0.45±0.12 | ≤16 | 0.90±0.12 |

Other sizes are available upon special order.

###### CB-GSRT

###### GREAT SHRINKING RATIO HEAT-SHRINKABLE TUBING

CB-GSRT tubes have the same property as CB-HFT tubing, besides its great shrink ratio. The tubing may be used for protection and marking of special shaped objects.

Specifications

| Item |  | Specifications Requirements |
| --- | --- | --- |
| Temperature Rating (℃) |  | -55～125 |
| Radial Shrinking Ratio (%) |  | ≥50 |
| Longitudinal Change (%) |  | ≤15 |
| Tensile Strength (Mpa) |  | ≥10.4 |
| Ultimate Elongation (%) |  | ≥200 |
| Aging in Circulating-air Oven |  | 158.0±1.0℃, 168hrs |
| After Aging | Tensile Strength (Mpa) | ≥7.28 |
|  | Ultimate Elongation (%) | ≥100 |
| Volume Resistivity (Ω cm) |  | 1014 |
| Dielectric Strength (KV/mm) |  | ≥15 |
| Flammability |  | VW-1 |
| Concentricity (%) |  | ≥65 |

Size

| Size (IN) | As Supplied (mm) |  | After Recovery (mm) |  |
| --- | --- | --- | --- | --- |
|  | Min.Inside Diameter | Nominal Wall-thickness | Max.Inside Diameter | Wall-thickness |
| 1/16 | 1.6 | 0.15 | 0.5 | 0.45 |
| 1/8 | 3.2 | 0.18 | 1.0 | 0.55 |
| 3/16 | 4.8 | 0.20 | 1.5 | 0.60 |
| 1/4 | 6.4 | 0.22 | 2.0 | 0.65 |
| 3/8 | 9.5 | 0.25 | 3.0 | 0.75 |
| 1/2 | 12.7 | 0.25 | 4.0 | 0.80 |
| 3/4 | 19.1 | 0.35 | 6.0 | 0.90 |
| 1 | 25.4 | 0.45 | 8.0 | 1.00 |
| 11/2 | 39.0 | 0.50 | 13.0 | 1.25 |

Other sizes are available upon special order.

CB-HRT

HEAT-RESISTING HEAT－SHRINKABLE TUBING

CB-HRT is a heat-resisting polyolefin heat-shrinkable tubing which is flexible, insulation and resistant to common fluids and solvents. This tubing  could be used for electrical insulation and strain relief of components that are exposed to high temperature. This tubing meets UL224 requiments.

Specifications

| Item |  | Specifications |
| --- | --- | --- |
| Shrink Temperature (℃) |  | 120 |
| Temperature Rating (℃) |  | 150 |
| Radial Shrinking Ratio (%) |  | ≥50 |
| Longitudinal Change (%) |  | ≤5 |
| Tensile Strength (Mpa) |  | ≥10.4 |
| Ultimate Elongation (%) |  | ≥200 |
| Aging in Circulating-air Oven |  | 180.0±1.0℃, 168hrs |
| After aging | Tensile Strength (Mpa) | ≥7.3 |
|  | Ultimate Elongation (%) | ≥100 |
| Concentricity (%) |  | ≥65 |
| Volume Resistivity (Ω cm) |  | ≥1014 |
| Dielectric Strength (KV/mm) |  | ≥15 |
| Water Absorption (%) |  | <0.4 |
| Copper Corrosion |  | No corrosion |

Size

| Size | As Supplied (mm) |  | After Recovery (mm) |  |
| --- | --- | --- | --- | --- |
|  | Inside Diameter | Wall-thickness | Inside Diameter | Wall-thickness |
| φ0.8 | 1.3±0.2 | 0.15±0.05 | ≤0.45 | 0.28±0.05 |
| φ1.0 | 1.5±0.2 | 0.18±0.05 | ≤0.6 | 0.30±0.05 |
| φ1.5 | 2.0±0.2 | 0.18±0.05 | ≤0.8 | 0.32±0.05 |
| φ2.0 | 2.5±0.2 | 0.18±0.05 | ≤1.00 | 0.35±0.05 |
| φ2.5 | 3.0±0.2 | 0.20±0.05 | ≤1.25 | 0.38±0.05 |
| φ3.0 | 3.5±0.3 | 0.20±0.05 | ≤1.5 | 0.38±0.05 |
| φ3.5 | 4.0±0.3 | 0.20±0.05 | ≤1.75 | 0.38±0.05 |
| φ4.0 | 4.5±0.3 | 0.23±0.05 | ≤2.0 | 0.45±0.05 |
| φ4.5 | 4.8±0.3 | 0.23±0.05 | ≤2.25 | 0.45±0.05 |
| φ5.0 | 5.5±0.3 | 0.23±0.05 | ≤2.5 | 0.45±0.05 |
| φ6.0 | 6.5±0.4 | 0.25±0.05 | ≤3.0 | 0.50±0.05 |
| φ6.5 | 7.0±0.4 | 0.25±0.05 | ≤3.0 | 0.52±0.05 |
| φ7.0 | 7.5±0.4 | 0.30±0.08 | ≤3.5 | 0.60±0.05 |
| φ8.0 | 8.5±0.3 | 0.30±0.08 | ≤4.0 | 0.60±0.08 |
| φ9.0 | 9.5±0.4 | 0.30±0.08 | ≤4.5 | 0.60±0.08 |
| φ10 | 10.5±0.5 | 0.30±0.08 | ≤5.0 | 0.60±0.08 |
| φ11 | 11.5±0.5 | 0.30±0.08 | ≤5.5 | 0.60±0.08 |
| φ12 | 12.5±0.5 | 0.30±0.08 | ≤6.0 | 0.60±0.08 |
| φ13 | 13.5±0.5 | 0.36±0.12 | ≤6.5 | 0.65±0.12 |
| φ14 | 14.5±0.5 | 0.36±0.12 | ≤7.0 | 0.65±0.12 |
| φ15 | 15.5±0.5 | 0.36±0.12 | ≤7.5 | 0.65±0.12 |
| φ16 | 16.5±0.5 | 0.36±0.12 | ≤8.0 | 0.70±0.12 |
| φ17 | 17.5±0.5 | 0.36±0.12 | ≤8.5 | 0.70±0.12 |
| φ18 | 18.7±0.5 | 0.40±0.15 | ≤9.0 | 0.75±0.12 |
| φ20 | 20.6±0.6 | 0.40±0.15 | ≤10.0 | 0.80±0.12 |
| φ22 | 22.7±0.6 | 0.40±0.15 | ≤11.0 | 0.80±0.12 |
| φ25 | 25.5±0.7 | 0.45±0.15 | ≤12.5 | 0.90±0.12 |
| φ28 | 29.2±0.7 | 045±0.15 | ≤14.0 | 0.90±0.12 |
| φ30 | 31.0±0.7 | 0.45±0.15 | ≤15.0 | 0.90±0.12 |
| φ35 | ≥35 | 0.50±0.15 | ≤19 | 1.00±0.30 |
| φ40 | ≥40 | 0.50±0.15 | ≤21 | 1.00±0.30 |
| φ50 | ≥50 | 0.50±0.15 | ≤27 | 1.00±0.30 |
| φ55 | ≥55 | 0.50±0.15 | ≤28 | 1.00±0.30 |

Size in Inch

| SIZE (in inch) | As supplied in mm |  | After Recovery (mm) |  |
| --- | --- | --- | --- | --- |
|  | MIN ID (in mm) | WALL (in mm) | MIN ID (in mm) | WALL (in mm) |
| 3/64 | 1.2 | 0.18±0.05 | ≤0.6 | 0.30±0.05 |
| 1/16 | 1.6 | 0.18±0.05 | ≤0.8 | 0.32±0.05 |
| 3/32 | 2.4 | 0.18±0.05 | ≤1.00 | 0.35±0.05 |
| 1/8 | 3.2 | 0.20±0.05 | ≤1.5 | 0.38±0.05 |
| 3/16 | 4.8 | 0.23±0.05 | ≤2.0 | 0.45±0.05 |
| 1/4 | 6.4 | 0.25±0.05 | ≤3.0 | 0.50±0.05 |
| 3/8 | 9.5 | 0.30±0.08 | ≤4.5 | 0.60±0.08 |
| 1/2 | 12.7 | 0.30±0.08 | ≤6.0 | 0.60±0.08 |
| 3/4 | 19.1 | 0.40±0.12 | ≤10.0 | 0.75±0.12 |
| 1 | 25.4 | 0.45±0.12 | ≤12.5 | 0.90±0.12 |
| 1–1/4 | 31.8 | 0.45±0.12 | ≤15.0 | 0.90±0.12 |
| 1–1/2 | 38.1 | 0.50±0.15 | ≤21 | 1.00±0.30 |
| 2 | 50.8 | 0.50±0.15 | ≤27 | 1.00±0.30 |

CB-TT   PTFE TUBING

CB-TT PTFE tubing is of high temperature (260℃) resistance, corrosion resistance, excellence insulation and mechanical strength properties. The tubing is being applied widely in industries of electrical, computer, chemical, high temperature areas, aerospace, military and transmission system etc, the product gained the UL recognition  (File No: E180908). All are F mark.

Rated Voltage:  300V/600V

Testing Voltae:  2500V

Rated Temperature:  -80～200℃

Specification

| Item | Test Method | Unit | Specification Requirement |
| --- | --- | --- | --- |
| Specific Gravity | ASTM D792 | g/cm3 | 2.16 |
| Tensile strength | ASTM D638 | M Pa | 24.5 |
| Ultimate Elongation | ASTM D638 | % | 350 |
| Flexural Modulus | ASTM D790 | M Pa | 490 |
| Impact Strength | ASTM D256+23℃-54℃j/m |  | -No break- 107 |
| Hardness | ASTM D2240 | Shore D | 55 |
| Coefficient Of Dynamic Friction |  |  | 0.1 |
| Melting Point |  | ℃ | 327 |
| Service Temperature 20000h with 50% Retention Of Ultimate Elongation |  | ℃ | 260 |
| Flammability | UL-224 |  | VW-1 |
| Dieletric Constant At 103-106Hz | ASTM D150 |  | 2.1 |
| Dissipation Factor At 106Hz | ASTM D150 |  | 0.0002 |
| Arc Resistance | ASTMD495 (Stainless steel electrodes) | S | ﹥300 |
| Volume Resistivity | ASTM D257 | Ώ cm | ﹥1018 |
| Weather Resistance | “Weather-o-meter”(2000h) |  | No break |
| Solvent Resistance | ASTM D543 |  | Excellent |
| Chemical Resistance | ASTM D543 |  | Excellent |

Size

| PTFE Insulation Tubing |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Size | ID（㎜） |  |  | OD（㎜） |  |  |
| AWG | MIN | NOR | MAX | S-TYPE | T-TYPE | L-TYPE |
| 30 | 0.25 | 0.30 | 0.38 | 0.76 | 0.76 | 0.60 |
| 28 | 0.33 | 0.38 | 0.46 | 0.84 | 0.84 | 0.68 |
| 26 | 0.41 | 0.46 | 0.53 | 0.92 | 0.92 | 0.76 |
| 24 | 0.51 | 0.56 | 0.66 | 1.16 | 1.06 | 0.86 |
| 23 | 0.58 | 0.66 | 0.74 | 1.26 | 1.16 | 0.96 |
| 22 | 0.66 | 0.71 | 0.81 | 1.31 | 1.21 | 1.01 |
| 21 | 0.74 | 0.81 | 0.89 | 1.41 | 1.31 | 1.11 |
| 20 | 0.81 | 0.86 | 0.97 | 1.66 | 1.46 | 1.16 |
| 19 | 0.91 | 0.96 | 1.07 | 1.76 | 1.56 | 1.26 |
| 18 | 1.01 | 1.07 | 1.17 | 1.87 | 1.67 | 1.37 |
| 17 | 1.14 | 1.19 | 1.32 | 1.99 | 1.79 | 1.49 |
| 16 | 1.29 | 1.34 | 1.47 | 2.14 | 1.94 | 1.64 |
| 15 | 1.45 | 1.50 | 1.65 | 2.30 | 2.10 | 1.80 |
| 14 | 1.62 | 1.68 | 1.83 | 2.48 | 2.28 | 2.08 |
| 13 | 1.83 | 1.93 | 2.05 | 2.73 | 2.53 | 2.33 |
| 12 | 2.05 | 2.16 | 2.31 | 2.96 | 2.77 | 2.56 |
| 11 | 2.31 | 2.41 | 2.57 | 3.21 | 3.01 | 2.81 |
| 10 | 2.59 | 2.69 | 2.84 | 3.49 | 3.29 | 3.09 |
| 9 | 2.90 | 3.00 | 3.15 | 4.00 | 3.76 | 3.40 |
| 8 | 3.28 | 3.38 | 3.53 | 4.38 | 4.14 | 3.78 |
| 7 | 3.65 | 3.76 | 3.94 | 4.76 | 4.52 | 4.16 |
| 6 | 4.11 | 4.22 | 4.41 | 5.22 | 4.98 | 4.72 |
| 5 | 4.62 | 4.72 | 4.95 | 5.72 | 5.48 | 5.22 |
| 4 | 5.18 | 5.28 | 5.53 | 6.28 | 6.04 | 5.78 |
| 3 | 5.81 | 5.94 | 6.20 | 6.94 | 6.70 | 6.44 |
| 2 | 6.55 | 6.68 | 6.93 | 7.68 | 7.44 | 7.18 |
| 1 | 7.34 | 7.46 | 7.75 | 8.46 | 8.22 | 7.96 |
| 0 | 8.26 | 8.38 | 8.69 | 9.38 | 9.14 | 8.88 |

Other sizes are available upon special order.

CB-300/CB-600 PVC TUBING

PVC tubing is a flexible flame-retardant not heat-shrinkable tubing which has excellent electrical and physical performances, and outstanding acid fastness and corrosion resistivity. This tubing is suitable for insulation purpose of electronics, automobil, terminal lugs, small electrical parts, lead wires of toy motors and transformers etc. The product is UL recognition and the file No is E180908 for black, and E250610 for clear. All are F mark.

Specification

| Item |  | Specifications |
| --- | --- | --- |
| Temperature Rating （℃） |  | 105 |
| Longitudinal Change |  | ≤±5% |
| Tensile Strength （MPa） |  | ≥10.4 |
| Ultimate Elongation （%） |  | ≥100 |
| Aging in Circulating-air Oven |  | 136.0±1.0℃, 168hrs |
| After aging | Tensile Strength (Mpa) | ≥7.3 |
|  | Ultimate Elongation （%） | ≥100 |
| Potential Rating (V) |  | 300V, 600V |
| Volume Resistivity (Ω cm) |  | ≥1010 |
| Dielectric Strength (V) |  | 2500（60s）,No breakdown |
| Corrosion of Bare Copper |  | No corrosion |
| Heat Shock |  | No cracking |
| Cold Bend |  | No cracking |

Size

| AWG size | Inside diameter (mm) | Average Wall-thickness (mm) |  |
| --- | --- | --- | --- |
|  |  | For CB-300 | For CB-600 |
| 5/8 | 16.0 | 0.85±0.18 | 0.85±0.18 |
| 9/16 | 14.3 |  |  |
| 1/2 | 12.7 | 0.70±0.15 | 0.70±0.15 |
| 7/16 | 11.1 |  |  |
| 3/8 | 9.53 |  |  |
| 5/16 | 7.92 |  |  |
| 0# | 8.38 | 0.55±0.1 |  |
| 1# | 7.47 |  |  |
| 2# | 6.68 |  |  |
| 3# | 5.94 |  |  |
| 4# | 5.28 |  |  |
| 5# | 4.72 |  |  |
| 6# | 4.22 |  |  |
| 7# | 3.87 |  |  |
| 8# | 3.38 |  |  |
| 9# | 3.00 |  |  |
| 10# | 2.69 | 0.45±0.1 |  |
| 11# | 2.41 |  |  |
| 12# | 2.16 |  |  |
| 13# | 1.93 |  |  |
| 14# | 1.68 |  |  |
| 15# | 1.50 |  |  |
| 16# | 1.34 |  |  |
| 17# | 1.19 |  |  |
| 18# | 1.07 |  | 0.55±0.1 |
| 19# | 0.96 |  |  |
| 20# | 0.86 |  |  |
| 21# | 0.79 |  |  |

Inside Diameter tolerance ±5%

Other sizes are available upon special order.

PET heat shrinkable tubing

PET tubing is free halogen and more friendly environment. It does not contain Pb,Hg,Cd and other heavy metal.

Specification

| Inspected item | Unit | Requirement |
| --- | --- | --- |
| Appearance |  | Without feculence |
| Bend (280mm) | mm | At or above size 8.0mm < 3.0 At or under size 10.0mm < 3.5 |
| Density | Kg/L | 1.3—1.4 |
| Tensile strength | N/m2 | 5.0*107---10.0*107 |
| Ultimate elongation rate | % | 200---350 |
| Absorbation (water) | % | < 2.0% |
| Dielectronic strength | Kv/mm | > 80 |
| Resistivity | Ω | > 109 |
| Volume resistivity | Ω.cm | > 1014 |
| Operating temperature range | ℃ | -40℃ — +130℃ |

| Size | Width (mm) | Thickness (×0.01mm) | Shrink Ratio (%) | Lognitudinal ratio (%) | Lognitudinal ratio (180±2) ℃ ×15 min |
| --- | --- | --- | --- | --- | --- |
| φ4 | 7.1±0.2 | 8.0±1.0 | 48±2 | 8±2 | 12±3 |
| φ5 | 9.1±0.2 | 8.0±1.0 | 48±2 | 8±2 | 12±3 |
| φ6 | 10.6±0.2 | 8.0±1.0 | 48±2 | 8±2 | 12±3 |
| φ6.3 | 11.0±0.2 | 8.0±1.0 | 48±2 | 8±2 | 12±3 |
| φ8 | 14.0±0.2 | 10.0±1.0 | 48±2 | 8±2 | 12±3 |
| φ10 | 17.0±0.2 | 10.0±1.0 | 48±2 | 8±2 | 12±3 |
| φ13 | 22.0±0.3 | 10.0±1.0 | 48±2 | 8±2 | 12±3 |
| φ14.8 | 25.0±0.3 | 10.5±1.5 | 48±2 | 8±2 | 12±3 |
| φ16 | 27.1±0.3 | 10.5±1.5 | 48±2 | 8±2 | 12±3 |
| φ18 | 3.02±0.3 | 10.5±1.5 | 48±2 | 8±2 | 12±3 |
| φ22 | 36.3±0.3 | 11.0±2.0 | 48±2 | 8±2 | 12±3 |
| φ25 | 41.3±0.3 | 11.0±2.0 | 48±2 | 8±2 | 12±3 |
| φ30 | 49.0±0.3 | 11.0±2.0 | 48±2 | 8±2 | 12±3 |
| φ35 | 56.6±0.3 | 11.0±2.0 | 48±2 | 8±2 | 12±3 |
| Remark: any size fromφ4.0—φ35.0 can be produced on customers’requirement. |  |  |  |  |  |

CB-101 HEAT－SHRINKABLE TUBING

CHANGBAO-101 tubing is a highly flexible-polyolefin non-flame-retardant heat-shrinkable tubing which is available in many high glossy colors and in high clarity clear material. This tubing has low shrink temperature of 90℃. CHANGBAO -101 may be applied for marking, lighting, automobile antenna etc.

Specifications

| Item |  | Specifications |
| --- | --- | --- |
| Shrink Temperature(℃) |  | 90 |
| Operating Temperature Range(℃) |  | -55～105 |
| Radial Shrinking Ratio(%) |  | ≥50 |
| Longitudinal Change(%) |  | ≤±5 |
| Tensile Strength(MPa) |  | ≥10.4 |
| Ultimate Elongation (%) |  | ≥200 |
| Aging in Circulating-air Oven |  | 136.0±1.0℃, 168hrs |
| After Aging | Tensile Strength(MPa) | ≥7.28 |
|  | Ultimate Elongation (%) | ≥100 |
| Volume Resistivity(Ω cm) |  | 1014 |
| Dielectric Strength(KV/mm) |  | ≥15 |
| Concentricity(%) |  | ≥6 |

Size

| Size | As Supplied(mm) |  | After Recovery(mm) |  |
| --- | --- | --- | --- | --- |
|  | Inside Diameter | Wall-thickness | Inside Diameter | Wall-thickness |
| φ0.8 | 1.3±0.2 | 0.20±0.05 | ≤0.40 | 0.40±0.05 |
| φ1.0 | 1.5±0.2 | 0.20±0.05 | ≤0.55 | 0.40±0.05 |
| φ1.5 | 2.0±0.2 | 0.20±0.05 | ≤0.75 | 0.42±0.05 |
| φ2.0 | 2.5±0.2 | 0.20±0.05 | ≤1.0 | 0.44±0.05 |
| φ2.5 | 3.0±0.2 | 0.22±0.05 | ≤1.25 | 0.47±0.05 |
| φ3.0 | 3.5±0.2 | 0.25±0.05 | ≤1.5 | 0.50±0.05 |
| φ3.5 | 4.0±0.3 | 0.25±0.05 | ≤1.75 | 0.50±0.05 |
| φ4.0 | 4.5±0.3 | 0.25±0.05 | ≤2.0 | 0.50±0.05 |
| φ4.5 | 4.8±0.3 | 0.25±0.05 | ≤2.0 | 0.52±0.05 |
| φ5.0 | 5.5±0.3 | 0.25±0.05 | ≤2.5 | 0.52±0.05 |
| φ6.0 | 6.5±0.3 | 0.25±0.05 | ≤3.0 | 0.52±0.05 |
| φ6.5 | 6.8±0.3 | 0.30±0.05 | ≤3.0 | 0.60±0.05 |
| φ7.0 | 7.5±0.3 | 0.30±0.05 | ≤3.5 | 0.60±0.05 |
| φ8.0 | 8.5±0.3 | 0.36±0.08 | ≤4.0 | 0.70±0.08 |
| φ9.0 | 9.5±0.3 | 0.36±0.08 | ≤4.5 | 0.70±0.08 |
| φ10 | 10.5±0.4 | 0.36±0.08 | ≤5.0 | 0.70±0.08 |
| φ11 | 11.5±0.4 | 0.36±0.08 | ≤5.5 | 0.70±0.08 |
| φ12 | 12.5±0.4 | 0.36±0.08 | ≤6.0 | 0.70±0.08 |
| φ13 | 13.5±0.4 | 0.36±0.12 | ≤6.5 | 0.70±0.12 |
| φ14 | 14.5±0.4 | 0.36±0.12 | ≤7.0 | 0.70±0.12 |
| φ15 | 15.5±0.4 | 0.36±0.12 | ≤7.5 | 0.70±0.12 |
| φ16 | 16.5±0.4 | 0.36±0.12 | ≤8.0 | 0.72±0.12 |
| φ17 | 17.5±0.4 | 0.36±0.12 | ≤8.5 | 0.77±0.12 |
| φ18 | 18.7±0.5 | 0.40±0.12 | ≤9.0 | 0.77±0.12 |
| φ20 | 20.6±0.8 | 0.40±0.12 | ≤10.0 | 0.80±0.12 |
| φ22 | 22.7±0.8 | 0.46±0.12 | ≤11.0 | 0.90±0.12 |
| φ25 | 25.5±0.8 | 0.46±0.12 | ≤12.5 | 0.90±0.12 |
| φ28 | 29.2±0.8 | 046±0.12 | ≤14.0 | 0.90±0.12 |
| φ30 | 31.0±0.8 | 0.46±0.12 | ≤15.0 | 1.00±0.12 |
| φ35 | ≥35 | 0.50±0.15 | ≤19 | 1.00±0.30 |
| φ40 | ≥40 | 0.50±0.15 | ≤21 | 1.00±0.30 |
| φ50 | ≥50 | 0.50±0.15 | ≤27 | 1.00±0.30 |
| φ55 | ≥55 | 0.50±0.15 | ≤28 | 1.00±0.30 |
| φ60 | ≥60 | 0.50±0.15 | ≤31 | 1.00±0.30 |

CB-301 HEAT－SHRINKABLE TUBING

CHANGBAO-301 tubing is made from polyethylene which has brilliant resistant to common fluids, solvents, acids, alkalis and oils and excellent insulation. It may be used in field of electronics, mobiles and aerospace etc, such as automobile oil pipes, refrigerator cooling pipe etc.

Specifications

| Item |  | Specifications |
| --- | --- | --- |
| Shrink Temperature(℃) |  | 120 |
| Operating Temperature Range(℃) |  | -55～105 |
| Radial Shrinking Ratio(%) |  | ≥50 |
| Longitudinal Change(%) |  | ≤±5 |
| Tensile Strength(MPa) |  | ≥10.4 |
| Ultigation Elongation(%) |  | ≥200 |
| Aging in Circulating-air Oven |  | 136.0±1.0℃, 168hrs |
| After Aging | Tensile Strength(MPa) | ≥7.28 |
|  | Ultimate Elongation(%) | ≥100 |
| Volume Resistivity(Ω cm) |  | ≥1015 |
| Dielectric Strength(KV/mm) |  | ≥25 |
| Concentricity(%) |  | ≥6 |

Size

| Size | As Supplied (mm) |  | After Recovery(mm) |  |
| --- | --- | --- | --- | --- |
|  | Inside Diameter | Wall-thickness | Inside Diameter | Wall-thickness |
| φ1.5 | 2.0±0.2 | 0.20±0.05 | ≤0.75 | 0.42±0.05 |
| φ2.0 | 2.5±0.2 | 0.20±0.05 | ≤1.0 | 0.44±0.05 |
| φ2.5 | 3.0±0.2 | 0.22±0.05 | ≤1.25 | 0.47±0.05 |
| φ3.0 | 3.5±0.2 | 0.25±0.05 | ≤1.5 | 0.50±0.05 |
| φ3.5 | 4.0±0.3 | 0.25±0.05 | ≤1.75 | 0.50±0.05 |
| φ4.0 | 4.5±0.3 | 0.25±0.05 | ≤2.0 | 0.50±0.05 |
| φ4.5 | 4.8±0.3 | 0.25±0.05 | ≤2.0 | 0.52±0.05 |
| φ5.0 | 5.5±0.3 | 0.25±0.05 | ≤2.5 | 0.52±0.05 |
| φ6.0 | 6.5±0.3 | 0.25±0.05 | ≤3.0 | 0.52±0.05 |
| φ6.5 | 6.8±0.3 | 0.30±0.05 | ≤3.0 | 0.60±0.05 |
| φ7.0 | 7.5±0.3 | 0.30±0.05 | ≤3.5 | 0.60±0.05 |
| φ7.0T | 7.5±0.3 | 0.40±0.05 | ≤3.5 | 0.80±0.05 |
| φ8.0 | 8.5±0.3 | 0.36±0.08 | ≤4.0 | 0.70±0.08 |
| φ9.0 | 9.5±0.3 | 0.36±0.08 | ≤4.5 | 0.70±0.08 |
| φ9.0T | 9.5±0.3 | 0.40±0.08 | ≤4.5 | 0.80±0.08 |
| φ10 | 10.5±0.4 | 0.36±0.08 | ≤5.0 | 0.70±0.08 |
| φ11 | 11.5±0.4 | 0.36±0.08 | ≤5.5 | 0.70±0.08 |
| φ12 | 12.5±0.4 | 0.36±0.08 | ≤6.0 | 0.70±0.08 |
| φ13 | 13.5±0.4 | 0.36±0.12 | ≤6.5 | 0.70±0.12 |
| φ14 | 14.5±0.4 | 0.36±0.12 | ≤7.0 | 0.70±0.12 |
| φ15 | 15.5±0.4 | 0.36±0.12 | ≤7.5 | 0.70±0.12 |
| φ16 | 16.5±0.4 | 0.36±0.12 | ≤8.0 | 0.72±0.12 |
| φ17 | 17.5±0.4 | 0.36±0.12 | ≤8.5 | 0.77±0.12 |
| φ18 | 18.7±0.5 | 0.40±0.12 | ≤9.0 | 0.77±0.12 |
| φ20 | 20.6±0.8 | 0.40±0.12 | ≤10.0 | 0.80±0.12 |
| φ22 | 22.7±0.8 | 0.46±0.12 | ≤11.0 | 0.90±0.12 |
| φ25 | 25.5±0.8 | 0.46±0.12 | ≤12.5 | 0.90±0.12 |
| φ28 | 29.2±0.8 | 046±0.12 | ≤14.0 | 0.90±0.12 |
| φ30 | 31.0±0.8 | 0.46±0.12 | ≤15.0 | 1.00±0.12 |

"T"-Products with special thickness.

Other sizes are available upon special order.

CB-150

Cross-linked, flame-retardant polyvinylidene fluoride heat-shrinkable tubing

Features & Benefits：

1) Flex

2) Clear

3) Thin Wa ll

4) Flame-retardant

5) Excellent oil and chemical resistance

Applications：

Especially suitable for applications abrasion resistance and cut-through resistance, or superior chemical and solvent properties performance . Provides electrical insulation and strain relief of multipin connectors and solder joints. Ideal for applications that require dense packing of components or visual inspection of covered components.

Technical Data：

| Proprty | Test Method | Unit | Typical Data |
| --- | --- | --- | --- |
| Specific Gravity | ASTM D792 | g/cm3 | 1.78 |
| Tensile strength | ASTM D2671 | M Pa | min30 |
| Elongation at break | ASTM D2671 | % | min150 |
| After Aging Elongation | 225℃,168h | % | min100 |
| Heat Shock | 275℃,4h | - | -No Cracking- |
| Cold Bend | -55℃,4h | - | -No Cracking- |
| Dielectric Strength | ASTM D2671 | kV/mm | min15.7 |
| Volume Resistivity | ASTM D257 | Ω.cm | min1013 |
| Flammability Rating | UL-224 | VW-1 | pass |

Special installation instructions：

full recovery temperature: 150°C

Product Dimensions

| Size | Inside Diameter |  | Recovered Wall Thickness** After Heating |
| --- | --- | --- | --- |
|  | Minimum Expanded as Supplied | Maximum Recovered After Heating |  |
| 3/64 | 1.2 [0.046] | 0.6 [0.023] | 0.25 ± 0.05 [0.010 ± 0.002] |
| 1/16 | 1.6 [0.063] | 0.8 [0.031] | 0.25 ± 0.05 [0.010 ± 0.002] |
| 3/32 | 2.4 [0.093] | 1.2 [0.046] | 0.25 ± 0.05 [0.010 ± 0.002] |
| 1/8 | 3.2 [0.125] | 1.6 [0.062] | 0.25 ± 0.05 [0.010 ± 0.002] |
| 3/16 | 4.8 [0.187] | 2.4 [0.093] | 0.25 ± 0.05 [0.010 ± 0.002] |
| 1/4 | 6.4 [0.250] | 3.2 [0.125] | 0.33 ± 0.05 [0.013 ± 0.002] |
| 3/8 | 9.5 [0.375] | 4.8 [0.187] | 0.33 ± 0.05 [0.013 ± 0.002] |
| 1/2 | 12.7 [0.500] | 6.4 [0.250] | 0.33 ± 0.05 [0.013 ± 0.002] |
| 4/3 | 19.1 [0.750] | 9.5 [0.375] | 0.43 ± 0.08 [0.017 ± 0.003] |
| 1 | 25.4 [1.000] | 12.7 [0.500] | 0.48 ± 0.08 [0.019 ± 0.003] |

**Wall thickness will be less if tubing recovery is restricted during shrinkage.

Standard Color: Clear (Natural)

*Other Color and sizes are available subject to special order

CB-175

Cross-linked, semi-rigid, flame-retardant polyvinylidene fluoride heat-shrinkable tubing

Features & Benefits：

1) Flame-retardant

2) Clear

3) Thin Wa ll

4) Semi-rigid

5) Excellent oil and chemical resistance

Applications：

Especially suitable for applications requiring hightemperature performance, outstanding abrasion resistance and cut-through resistance, or superior chemical and solvent properties. Provides electrical insulation and strain relief of multipin connectors and solder joints. Ideal for applications that require dense packing of components or visual inspection of covered components.

Technical Data：

| Proprty | Test Method | Unit | Typical Data |
| --- | --- | --- | --- |
| Specific Gravity | ASTM D792 | g/cm3 | 1.78 |
| Tensile strength | ASTM D2671 | M Pa | min34.5 |
| Elongation at break | ASTM D2671 | % | min150 |
| After Aging Elongation | 250℃,168h | % | min50 |
| Heat Shock | 300℃,4h | - | -No Cracking- |
| Cold Bend | -55℃,4h | - | -No Cracking- |
| Dielectric Strength | ASTM D2671 | kV/mm | min30 |
| Volume Resistivity | ASTM D257 | Ω.cm | min1013 |
| Flammability Rating | UL-224 | VW-1 | pass |

Special installation instructions：

Minimum full recovery temperature: 175°C [347°F]

Product Dimensions

| Size | Inside Diameter |  | Recovered Wall Thickness** After Heating |
| --- | --- | --- | --- |
|  | Minimum Expanded as Supplied | Maximum Recovered After Heating |  |
| 3/64 | 1.2 [0.046] | 0.6 [0.023] | 0.25 ± 0.05 [0.010 ± 0.002] |
| 1/16 | 1.6 [0.063] | 0.8 [0.031] | 0.25 ± 0.05 [0.010 ± 0.002] |
| 3/32 | 2.4 [0.093] | 1.2 [0.046] | 0.25 ± 0.05 [0.010 ± 0.002] |
| 1/8 | 3.2 [0.125] | 1.6 [0.062] | 0.25 ± 0.05 [0.010 ± 0.002] |
| 3/16 | 4.8 [0.187] | 2.4 [0.093] | 0.25 ± 0.05 [0.010 ± 0.002] |
| 1/4 | 6.4 [0.250] | 3.2 [0.125] | 0.33 ± 0.05 [0.013 ± 0.002] |
| 3/8 | 9.5 [0.375] | 4.8 [0.187] | 0.33 ± 0.05 [0.013 ± 0.002] |
| 1/2 | 12.7 [0.500] | 6.4 [0.250] | 0.33 ± 0.05 [0.013 ± 0.002] |
| 4/3 | 19.1 [0.750] | 9.5 [0.375] | 0.43 ± 0.08 [0.017 ± 0.003] |
| 1 | 25.4 [1.000] | 12.7 [0.500] | 0.48 ± 0.08 [0.019 ± 0.003] |
| 1 1/2 | 38.1 [1.500] | 19.1 [0.750] | 0.48 ± 0.08 [0.019 ± 0.003] |

**Wall thickness will be less if tubing recovery is restricted during shrinkage.

Standard Color: Clear (Natural)

*Other Color and sizes are available subject to special order

CB-2000

DUAL-WALL TUBING FOR AUTOMOTIVE METAL PIPE

Specially designed for use on industry standard metal pipes to provide protection for automotive metal pipes and fuel lines. This product is positioned on straight pipe lengths prior to the sencond end-nut fitting. This product can effectively protect the automotive metal pipes and fuel lines against any kinds of damages caused by friction, corrosion, and improves the safety of automotive.

FEATURES

- Good oil resistance

- Meets: SAE-AMS-DTL-23053

- Operating temperature range: -40-125℃

- Minimum full recovery temperature: 110℃

SPECIFICATION

| Property |  | Test Method | Standard | Typical Value |
| --- | --- | --- | --- | --- |
| Longitudinal shrinkage |  |  | 0-10% | -2% |
| Eccentricity |  | ASTM D 2671 | 20% | 10% |
| Tensile strength |  | ASTM D 2671 | 12PM(mm) | 14PM |
| Elongation bresk |  | ASTM D 2671 | 400% | 460% |
| Aiging in Circulating-air Oven |  | 158.0±1.0%, 168hrs |  |  |
| After aging | Tensile Strength (Mpa) |  | 12PM(mm) | 13PM |
|  | Ultimate Elongation (%) |  | 270% | 410% |
| Deformation resistance |  |  | 50%(min) | 82% |
| Impact resistance |  |  | No cracking at -35℃ | No cracking |
| Drop impact resistance |  | ASTM D 746 | No cracking | No cracking |
| Cold resistance |  | ASTM D 746 after 1hrs, at -35℃ | No cracking | No cracking |
| Stress cracking resistance |  | ASTM S 1693 50℃, 24HRS | No cracking | No cracking |
| Fluid resistance |  | ASTM D 2671 | No cracking after 72h at | No cracking |
|  |  |  | 25 for Sulphuric acid |  |
|  |  |  | (1.28 S.G0) |  |
|  |  |  | Sodium hydroxide (0.1N) |  |
|  |  |  | Moor vehicle |  |
|  |  |  | Unleaded petrol |  |

Size

| Standard Pipe Diameter (mm) | Inside Diameter | Wall thinckness | Ordering description |
| --- | --- | --- | --- |
|  | As supplied in mm | After recovery (mm) |  |
| 3.50 | 5.0 | 1.0 | CB2000-5 |
| 4.76 | 6.0 | 1.0 | CB2000-6 |
| 6.35 | 8.0 | 1.0 | CB2000-8 |
| 8.00 | 10.0 | 1.0 | CB2000-10 |
| 10.00 | 15.0 | 1.0 | CB2000-15 |
| 4.85 | 14.0 | 1.0 | CB2000-14 |

CB-UL

THSTULTRA LOW TEMPERATURE FLEXIBLE RUBBER TUBING

CB-UL THST tubing is manufactured with radiation cross-linked rubber. The specially materials make the tubing very flexible and shrink at very low temperature( the minimum shrink temperature is 32℃). It is suitable for using on or near delicate temperature-sensitive materials or in special environments.

- Temperature Rating: 65℃

- Minimum shrink temperature: 32℃

- Minimum fully recovery shrink temperature: 42℃

- Shrink rate: 1.5:1

Technical data

| Property | Test Method | Typical Date |
| --- | --- | --- |
| Tensile strength | ASTM D 2671 | >10.5 Mpa |
| Elongation at break | ASTM D 2671 | >200% |

Product Dimensions( mm/inch )

| Size (mm) | As supplied ID Minimum (mm) | After recovered |  |
| --- | --- | --- | --- |
|  |  | ID maximum (mm) | Nom. Wll thickness (mm) |
| 3/4 | 19.1 | 12.7 | 1.0 |

- The basic color is Black, the other color except clear are also available.

- The sepecil size is available on the requirement.

http://prowest.ua

http://prowest.ws